## Slide 1: Plastics

## Slide 2: Monomer
Monomer
These are repeating basic units of a polymer.

## Slide 3: Polymers
These are materials whose molecules are made of repeating individual units called monomers. So polymers are high molecular weight compounds formed by the combination of a large number of one or more types of molecules of low molecular weight.

## Slide 4: Synthetic plastics
These are synthetic organic materials which are rigid in their final useful form, but on some
stage of their manufacture under pressure and temperature can be made into different shapes.
They are made from synthetic resins. To some extent names of synthetic resins and plastics
are interchangeable, based on chemical change during their transition.

## Slide 5: Groups
Two main groups of synthetic resins which ultimately turn to plastics are
i) thermo setting resins
ii) thermo plastic resins.

## Slide 6: Thermosetting resins
These are molded under heat and pressure and held in the heat until set and then cooled. But on reheating it will not soften. Hence setting is irreversible

## Slide 7: Thermo plastic resins
These resins are molded under heat and pressure and then chilled. These on reheating will soften and can give new shape. Therefore they are reversible.
So thermosetting plastics are preferred if the article will be exposed to heat. The resin can be molded with out filler.
But commonly thermosetting resins are mixed with appreciable percentage of filler like wood flour, cellulose, cotton, asbestos, carbon black, mica etc.

## Slide 8: Difference between thermosetting and thermo plastic resins
Thermo setting Thermo plastic
1. Formed by condensation 1.Formed by addition Polymerization polymerization
2. Have three-dimensional 2. Have long
cross linked structure chain linear polymers

## Slide 9
3. Do not soften on heating 3. Softens on but can be charred heating on strong heating
4. Cannot be reshaped and reused 4. Can be softened, can be reshaped
                and reused by reheating

## Slide 10
5. Hard, strong and brittle 5. Weak, soft and brittle
6. Cannot be reclaimed from waste
6. Can be reclaimed from waste.

## Slide 11: Classification
Plastics are classified as follows
Synthetic resins
Cellulose derivative plastics
Natural resins
Protein products

## Slide 12: Raw materials classification
Based on the type of raw materials used for manufacture they are classified as
Those derived from coal tar products.
Those utilizing products of non-coal tar origin- this can be further classified as
  plastics based on cellulose and plants b) derived primarily from hydrocarbons of
petroleum, natural gas and acetylene
Urea resins
Those derived from rubber and alkyl chlorides.

## Slide 13
Plastics and resins can be best arranged based on their general application.
thermosetting
thermoplastic
oil soluble
Protein products.

## Slide 14: Formation of synthetic resins
Resins are commonly formed from condensation and addition polymerization.

## Slide 15: Condensation polymerization
This involves the formation and elimination or splitting out a molecule of water from two different molecules followed by the union of two large remaining portions.
Example: Phenol-formaldehyde, urea- formaldehyde, phthalic anhydride- glycerol
Nylon 66
NH2(CH2)6NH2 + HOOC-(CH2)4 COOH → - (NH2(CH2)6NH-CO-(CH2)4 COOH)-
Monomer
Large number of monomers joins to form the polymer.

## Slide 16: Addition polymerization
Here polymerization takes place though the double bond, no elimination of substance.
Example : PVC, polythene.
CH2= CH2 + CH2=CH2 →CH3-CH2-CH=CH2
Monomer dimer
CH3-CH2-CH=CH2 + CH2= CH2 → CH3-CH2-CH2-CH2CH=CH2
Dimer monomer trimer
Usually condensation polymerization gives thermosetting resins and addition polymerization thermoplastic resins.

## Slide 17: Manufacture of synthetic resins
During the manufacture process mix two liquids or a solid and a liquid , heat them together to produce the reaction. Then remove water. Then continue heating with or without addition of monomers until a test solution shows proper melting point and viscosity for the polymer. Length of heating, catalyst and temperature influences the end product. Depth of color depends partly on the degree of purity of raw material. Darker the raw material, darker will be the product. Commonly inexpensive raw materials like urea, formaldehyde, phenol, glycerin, acetylene etc are used for preparation.

## Slide 18: General notes on manufacture
In addition to raw material the following chemicals are also added.
Binder: This is added for binding the resin. A resin or a cellulose derivative is added as a binder.
Filler: Cellulose, wood flour, cotton fiber, asbestos, mica etc.

## Slide 19
Plasticizers: These are substances added to alter the property of cellulose derivatives and other thermoplastic resins to produce tough and resilient product. Examples are camphor, adipicacid etc. Usually they are 10% weight of finished product.
Dyes and pigments: These are added as colouring agents.
Catalysts: Thermosetting resins may use either an acidic or basic catalyst depending up on desired properties of the resin.
Lubricants: Stearates, metallic soaps.

## Slide 20: Polythene or polyethylene
This is produced by the polymerization of ethylene. Ethylene gas is liquefied under pressure of 1500atm and pumped at 150-250oC during which polymerization takes place. Catalytic effect is given by 0.08% O2.
CH2=CH2 → -(CH2-CH2-CH2-CH2)n -
Polythene
Other catalysts used are benzoyl peroxide, hydrogen peroxide and azo compounds.

## Slide 21: Properties
It is a white rigid waxy solid.
It is a thermoplastic and lighter than water.
It has good moisture resistance and electrical resistance so it is used as an insulator.

## Slide 22: Uses
Used for injection moulding and extrusion material. Polythene mouldings are used in bottle caps, toys, domestic articles, covering wires, cables and for making pipes for cold water plumbing and chemical plants.

## Slide 23: Polystyrene
Prepared by the polymerization of styrene. The catalyst used is bezoylperoxide
C6H5-CH2-CH2 → -(CH2-CH2- - - - CH2-CH)n -
styrene C6H5 C6H5

## Slide 24: Uses
Used for injection molding of articles like toys , combs, buttons, electrical parts, battery cases, radio, TV and refrigerator parts.

## Slide 25: PVC
Polyvinylchloride is prepared by the polymerization of vinyl chloride at 40oC.
Vinyl chloride is prepared by heating acetylene and HCl at60-80oC, metal chloride is used as catalyst.
CH≡CH + HCl → CH2=CHCl
Vinyl chloride
CH2=CHCl → -(CH2-CHCl)n-
PVC
The polymerization is carried out in presence of water , benzyolperoxide.

## Slide 26: Properties
Non-inflammable, Thermoplastic, Odorless, taste less, chemically inert, insoluble in cold solvents, soluble in hot chlorinated hydrocarbons like ethylene chloride. Stable to light and heat.

## Slide 27: Bakelite
This is a phenol- formaldehyde resin. It is prepared from the polymerization of phenol and formaldehyde.
Uses
For making electrical insulation, cycle parts, automobile parts etc and as a varnish.